[image: image1.jpg]AR





	
	Date
	Norm
	Lab
	Result

	Commercial Name
	01.02.2022
	EN 12440 – 2018
	Michael Böttner
	„LOLASHENI GREY“

	Petrography
	02.06.2021
	EN 12407 – 2019
	CET – 1860 L
	Hornfels from Georgia, Kutaisi, Orpiri-Koka

	Description
	01.02.2022
	EN 12440 – 2018
	Michael Böttner
	Grey-anthrazite, medium cristallin, homogenic rock, some white & grey cristals, but mainly anthrazite; no apparent textures

	Water absorption by open porosity
	07.05.2021
	EN 1936 – 2007
	CET – 1860 L
	0,3%

	Density
	12.05.2021
	EN 1936 – 2007
	CET – 1860 L
	2740 kg/m³

	Compressive strength
	11.05.2021
	EN 1926 – 2007
	CET – 1860 L
	197 Mpa

	Flexural strength
	11.05.2021
	EN 12372 – 2007
	CET – 1860 L
	23 Mpa

	Water absorption under atmospheric pressure
	14.05.2021
	EN 13755 – 2008
	CET – 1860 L
	0,2%

	Abrasive resistance
	14.05.2021
	EN 14157A – 2017
	CET – 1860 L
	15,5 mm

	Freeze-Thaw resistance – compressive strength
	15.06.2021
	EN 1926 – 2007

EN 12371 – 2010


	CET – 1860 L
	183 Mpa

	Placing on market by
	01.02.2022
	
	Company:

Lolasheni LLC
	www.lolasheni.ge 
ID.N°: 205275183











This Data Sheet and the withgoing CE-Marking have been dressed by the Material-Lab for Natural Stones, Mineral Ressources and Concrete and Concrete-Ware, CET, Isera(TN)-Italy.


Processed under supervision and collaboration of Dr.Mag.Michael Böttner, Laboratorio Petrographico, Sluderno(BZ)-Italy.











TECHNICAL DATA SHEET





“LOLASHENI DARK”





Hornfels from Georgia, Imereti, Kutaisi, Orpiri-Koka





1860 L











PAGE  
1

